About ASTM

ASTM International is one of the largest voluntary standards development organizations in the world-a trusted source for technical standards for materials, products, systems, and services. Known for their high technical quality and market relevancy, ASTM International standards have an important role in the information infrastructure that guides design, manufacturing and trade in the global economy.

ASTM D5511

Significance and Use

Biodegradation of a plastic within a high-solids anaerobic digestion unit is an important phenomenon because it will affect the decomposition of other waste materials enclosed by the plastic and the resulting quality and appearance of the compost after an anaerobic digestion process. Biodegradation of plastics could allow for the safe disposal of these plastics through aerobic and anaerobic solid-waste-treatment plants. This procedure has been developed to permit the determination of the rate and degree of anaerobic biodegradability of plastic products when placed in a high-solids anaerobic digester for the production of compost from municipal solid waste.

Limitations—Because there is a wide variation in the construction and operation of anaerobic-digestion systems and because regulatory requirements for composting systems vary, this procedure is not intended to simulate the environment of any particular high-solids anaerobic-digestion system. However, it is expected to resemble the environment of a high-solids anaerobic-digestion process operated under optimum conditions. More specifically, the procedure is intended to create a standard laboratory environment that will permit a rapid and reproducible determination of the anaerobic biodegradability under high-solids digestion conditions.

1. Scope

1.1 This test method covers the determination of the degree and rate of anaerobic biodegradation of plastic materials in high-solids anaerobic conditions. The test materials are exposed to a methanogenic inoculum derived from anaerobic digesters operating only on pretreated household waste. The anaerobic decomposition takes place under high-solids (more than 30 % total solids) and static non-mixed conditions.

1.2 This test method is designed to yield a percentage of conversion of carbon in the sample to carbon in the gaseous form under conditions found in high-solids anaerobic digesters, treating municipal solid waste (1, 2, 3, 4). This test method may also resemble some conditions in biologically active landfills where the gas generated is recovered and biogas production is even actively promoted, for example, by inoculation (codeposition of anaerobic sewage sludge, anaerobic leachate recirculation), moisture control in the landfill (leachate recirculation), and temperature control (short-term injection of oxygen, heating of recirculated leachate) (5, 6, 7).

1.3 This test method is designed to be applicable to all plastic materials that are not inhibitory to the microorganisms present in anaerobic digesters operating on household waste.

1.4 The values given in SI units are to be regarded as the standard.

1.5 This test method is equivalent to ISO DIS15985.

1.6 This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use. Specific hazards are given in Section 8.

2. Referenced Documents

D1293 Test Methods for pH of Water

D1888 Test Methods for Particulate and Dissolved Matter, Solids, or Residue in Water

D2908 Practice for Measuring Volatile Organic Matter in Water by Aqueous-Injection Chromatography

D3590 Test Methods for Total Kjeldahl Nitrogen in Water

D4129 Test Method for Total and Organic Carbon in Water by High-Temperature Oxidation and by Coulometric Detection

D618 Practice for Conditioning Plastics for Testing

D883 Terminology Relating to Plastics

E260 Practice for Packed Column Gas Chromatography

E355 Practice for Gas Chromatography Terms and Relationships

212 Nitrogen Ammonia

2540 D Total Suspended Solids Dried at 103-105C

2540 E Fixed and Volatile Solids Ignited at 550C

ISO DIS 15985 Plastics- Determination of the Ultimate Anaerobic Biodegradability and Disintegration Under High-Solids Anaerobic-Digestion Conditions- Method by Analysis of Released Biogas

Index Terms

anaerobic biodegradation; anaerobic digestion; biodegradation; high-solids digestion; landfill; plastics test method; ICS Number Code 13.030.99 (Other standards related to wastes)

DOI: 10.1520/D5511-02

ASTM D5338

Significance and Use

Biodegradation of a plastic within a composting unit is an important phenomenon because it will affect the decomposition of other materials enclosed by the plastic and the resulting quality and appearance of the composted material. Biodegradation of plastics will also allow the safe disposal of these plastics through solid-waste composting plants. This procedure has been developed to permit the determination of the rate and degree of aerobic biodegradability of plastic products when placed in a controlled composting process.

Limitations—Because there is a wide variation in the construction and operation of composting systems and because regulatory requirements for composting systems vary, this procedure is not intended to simulate the environment of any particular composting system. However, it is expected to resemble the environment of a composting process operated under optimum conditions. More specifically, the procedure is intended to create a standard laboratory environment that will permit a rapid and reproducible determination of the aerobic biodegradability under controlled composting conditions.

1. Scope

1.1 This test method determines the degree and rate of aerobic biodegradation of plastic materials on exposure to a controlled-composting environment under laboratory conditions. This test method is designed to yield reproducible and repeatable test results under controlled conditions that resemble composting conditions. The test substances are exposed to an inoculum that is derived from compost from municipal solid waste. The aerobic composting takes place in an environment where temperature, aeration and humidity are closely monitored and controlled.

1.2 This test method is designed to yield a percentage of conversion of carbon in the sample to carbon dioxide. The rate of biodegradation is monitored as well.

1.3 This test method is designed to be applicable to all plastic materials that are not inhibitory to the microorganisms present in aerobic composting piles.

1.4 The values stated in SI units are to be regarded as the standard.

1.5 This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use. Specific hazard statements are given in Section 8.

1.6 This test method is equivalent to ISO 14852.

2. Referenced Documents

D1293 Test Methods for pH of Water

D1888 Test Methods for Particulate and Dissolved Matter, Solids, or Residue in Water

D2908 Practice for Measuring Volatile Organic Matter in Water by Aqueous-Injection Chromatography

D3590 Test Methods for Total Kjeldahl Nitrogen in Water

D4129 Test Method for Total and Organic Carbon in Water by High-Temperature Oxidation and Coulometric Detection

D618 Practice for Conditioning Plastics for Testing

D883 Terminology Relating to Plastics

E260 Practice for Packed Column Gas Chromatography

E355 Practice for Gas Chromatography Terms and Relationships

2540D Total Suspended Solids Dried at 103 to 105C

2540E Fixed and Volatile Solids Ignited at 550C

ISO14855 Plastics-Evaluation of the Ultimate Aerobic Biodegradability and Disintegration Under Controlled Composting Conditions-Method by Analysis of Released Carbon Dioxide

Index Terms

aerobic biodegradation; biodegradation; composting; plastics

DOI: 10.1520/D5338-98R03